10- W0.40Ta0.40Cr0.10Ti0.10 – HIP fast cooling – 1100C 6 weeks – Black Regions (Ti-rich)

1. Spot

FW: 80 μm, Mode: 15 kV - Image, WD: 7.5 mm, Detector: BSD Full, Time: 10/30/24 1:55 PM

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 22 | Ti | Titanium | 100.000 | 100.000 |

85 368 counts in 0:00:20 (4 227 c/s)

Disabled elements: Cs, Ho, Nb, Yb, Tm, Er, Eu, La, C, O, Si

2. Spot

FW: 80 μm, Mode: 15 kV - Image, WD: 7.5 mm, Detector: BSD Full, Time: 10/30/24 1:55 PM

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 22 | Ti | Titanium | 99.024 | 96.382 |
|  | 73 | Ta | Tantalum | 0.465 | 1.709 |
|  | 74 | W | Tungsten | 0.511 | 1.910 |

73 962 counts in 0:00:20 (3 669 c/s)

Disabled elements: Cs, Ho, Nb, Yb, Tm, Er, Eu, La, C, O, Si, Rb

3. Spot

FW: 94 μm, Mode: 15 kV - Image, WD: 7.5 mm, Detector: BSD Full, Time: 10/30/24 2:07 PM

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 22 | Ti | Titanium | 92.333 | 80.500 |
|  | 23 | V | Vanadium | 2.481 | 2.300 |
|  | 73 | Ta | Tantalum | 3.006 | 9.900 |
|  | 74 | W | Tungsten | 2.181 | 7.300 |

88 872 counts in 0:00:20 (4 401 c/s)

Disabled elements: Cs, Ho, Nb, Yb, Tm, Er, Eu, La, C, O, Sr, B, Si

4. Spot

FW: 94 μm, Mode: 15 kV - Image, WD: 7.5 mm, Detector: BSD Full, Time: 10/30/24 2:07 PM

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 22 | Ti | Titanium | 96.452 | 87.800 |
|  | 73 | Ta | Tantalum | 3.548 | 12.200 |

86 610 counts in 0:00:20 (4 288 c/s)

Disabled elements: Cs, Ho, Nb, Yb, Tm, Er, Eu, La, C, O, Sr, B, Si